## Slide 1
Vascular targeting of nanomedicines
Institut Galien Paris-Saclay
UMR CNRS 8612
Simona MURA
28 novembre 2024

## Slide 2
2
The scale of objects
2
Molecule
< 10 nm
Virus
20 -400 nm
Protein
10 -20 nm
Red blood cells
7 µm
Sand
100 μm - 5 mm
Nanometer
(10-9 meter)
Micrometer
(10-6 meter)
Millimeter
(10- 3 meter)
100 nm
1 nm
1000 nm
Bacteria
500 nm –10 μm
Hair
10 μm

## Slide 3
3
The scale of objects
3
Molecule
< 10 nm
Virus
20 -400 nm
Protein
10 -20 nm
Red blood cells
7 µm
Sand
100 μm - 5 mm
Nanometer
(10-9 meter)
Micrometer
(10-6 meter)
Millimeter
(10- 3 meter)
100 nm
1 nm
1000 nm
Polymer nanoparticle
Liposomes
Bacteria
500 nm –10 μm
Hair
10 μm

## Slide 4
Nanomedicines
Free drug
Traditional chemotherapy
Ligand
PEG
Nanoparticle
100 nm
Imaging
4
Vector size
Lipophilicity
Stability
Cytotropism
Size
Pka
Lipophilicity
Binding to plasma proteins
Biotransformations
Distribution
Alternative Distribution
Make the fate of a drug dependent from a carrier
The magic bullet

## Slide 5
5
Optimization of drug pharmacokinetics and biodistribution
Distribution
Tissues
Cells
D
Metabolization
Liver
M
Elimination
Kidneys
Gall bladder
E
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 6
6
Optimization of drug pharmacokinetics and biodistribution
Distribution
Tissues
Cells
D
Metabolization
Liver
M
Elimination
Kidneys
Gall bladder
E
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 7
7
Optimization of drug pharmacokinetics and biodistribution
Distribution
Tissues
Cells
D
Metabolization
Liver
M
Elimination
Kidneys
Gall bladder
E
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 8
Free drug
Nanoparticle
8
Nanomedicines
Protection from degradation
Increase intracellular penetration
Cell/tissue targeting
Overcome resistance
Traditional chemotherapy
Instability/metabolization
Limited intracellular accumulation
Lack of cell/tissue specificity
Induction of resistance phenomena
Make the fate of a drug dependent from a carrier
The magic bullet

## Slide 9
9
Different generations of nanomedicines
1st generation
3rd generation
2nd generation
Drug
Stealth/Long circulating
Surface functionalized
Stealth/Long circulating

## Slide 10
10
Different generations of nanomedicines
1st generation
3rd generation
2nd generation
Drug
Stealth/Long circulating
Surface functionalized
Stealth/Long circulating

## Slide 11
11
1st generation
Spleen
Kidneys
Liver
Nanoparticle uptake
by Kupffer cells
Rapid removal from the circulation
Macrophage uptake and liver accumulation
Macrophages
Endothelium
Plasma proteins
Internalization
Opsonization

## Slide 12
Hydrogen bonds
Electrostatic interactions
Hydrophobic interactions
Acid-base interactions
Hydration/solvation forces
Steric hindrance
Electrostatic repulsion
In vivo fate
Interactions in the biological medium_the protein corona

## Slide 13
13
Different generations of nanomedicines
1st generation
3rd generation
2nd generation
Drug
Stealth/Long circulating
Surface functionalized
Stealth/Long circulating

## Slide 14
14
Enhanced permeability
Stimulation of the blood vessel production
Important vascularization (blood supply)
Wide fenestrations, abnormal architectures
Accumulation of nanoparticles in
tumor and inflammed tissues
The enhanced permeability and retention effect (EPR)
Enhanced retention
Inefficient lymphatic drainage
2nd generation: long circulating

## Slide 15
15
The enhanced permeability and retention effect (EPR)
2nd generation: long circulating
Opsonization
Prolonged blood circulation
Non stealth NPs
Tumor
Inflammation
Stealth NPs

## Slide 16
16
Healthy tissue
Tumor tissue
S. Unezaki et al., International Journal of Pharmaceutics 1996, 144, 11
@24h
@ 24h
@ 48h
@ 30’
2nd generation: long circulating
S. Unezaki et al., International Journal of Pharmaceutics 1996, 144, 11

## Slide 17
17
Different generations of nanomedicines
1st generation
3rd generation
2nd generation
Drug
Stealth/Long circulating
Surface functionalized
Stealth/Long circulating

## Slide 18
18
Nanocarrier Behavior in the Circulation
diameter 10–50 μm
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 19
19
Nanocarrier Behavior in the Circulation
Microvasculature
Extended luminal surface area
Micrometer-scale vessel caliber
Low flow rate
Preferable target for endothelial nanomedicine
Tian GE et al., World J Stem Cells 2019; 11(12): 1104-1114 ; Jebari-Benslaiman S et al., Int. J. Mol. Sci. 2022, 23(6), 3346
Physiological
Pathological

## Slide 20
20
Shear-activated nanotherapeutics
Korin N et al., Science 2012, 337, 738– 742
2 µm
Microparticles
Nanoparticle release
Nanoparticles
High local shear stress
Stenotic and thrombosed vessels > 1000 dyne/m2
Normal vessel 70 dyne/cm2

## Slide 21
21
Containing fluorescent NPs
Coated with tissue plasminogen activator (tPA)
(~5 × 105 tPA molecules/micro-aggregate)
Arterial thrombus model
Direct exposure of the vessel wall to ferric chloride
Shear-activated nanotherapeutics
Korin N et al., Science 2012, 337, 738– 742

## Slide 22
22
SA-NTs
PBS
Shear-activated nanotherapeutics
Time to full vascular occlusion in FeCl-injured vessels
Korin N et al., Science 2012, 337, 738– 742
Fluorescently labeled platelets

## Slide 23
23
Nanocarrier Behavior in the Circulation
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Prolonged circulation versus targeting
Hydration Layer
Hydrophilic polymer
Poly(ethylene glycol)

## Slide 24
24
Nanocarrier Behavior in the Circulation
Ligand conjugation via PEG alleviates the masking effect.
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Prolonged circulation versus targeting
Hydration Layer
Hydrophilic polymer
Poly(ethylene glycol)

## Slide 25
25
Nanocarrier Behavior in the Circulation
Carrier geometry
Prolonged circulation of elongated objects
Uptake is modulated by the axis of particle binding to cell surface
Uncomplete internalization of disk-shaped particles contacting on their flat face
rounded end
flat face
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 26
26
Maksimenko A et al., PNAS 2014, 111, E217
Loop & train structure
100 nm
Geometry_elongated nanoparticles
Extended by the blood flow along streamlines

## Slide 27
27
Maksimenko A et al., PNAS 2014, 111, E217
Loop & train structure
Extended by the blood flow along streamlines
Geometry_elongated nanoparticles
Pharmacokinetics and biodistribution
100 nm

## Slide 28
28
Geometry_Long-circulating filomicelles
Filomicelles are self-assembled from di-block copolymers:
yellow/green: hydrophobic polymer
orange/blue : hydrophilic polymer
in vivo circulation for up to one week
Geng Y et al., Nat Nanotechnol 2007, 2, 249– 255

## Slide 29
29
Static conditions
Under flow, 25mm/s
Activated macrophages_24 h incubation
Phagocytosis of filomicelles is a strong function of filomicelles lenght
Long filomicelles flow past the cells
Small micelles and vesicles are captured
5 mm
Geng Y et al., Nat Nanotechnol 2007, 2, 249– 255
Geometry_Long-circulating filomicelles

## Slide 30
30
In vivo antitumor efficacy (murine lung cancer model)
Apoptosis
Tumor Volume
Geng Y et al., Nat Nanotechnol 2007, 2, 249– 255
Geometry_Long-circulating filomicelles

## Slide 31
31
Carrier Binding to Endothelium
anchors a carrier to endothelium in the area of interest
provides desirable subcellular addressing
not adversely affected by carrier binding
Adequate level of expression/localization
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Endothelial Determinants for Nanocarrier Targeting

## Slide 32
32
Carrier Binding to Endothelium
anchors a carrier to endothelium in the area of interest
provides desirable subcellular addressing
not adversely affected by carrier binding
Adequate level of expression/localization
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
ICAM-1
Fibroblasts
Muscle cells
Comparable levels of expression
Endothelial Determinants for Nanocarrier Targeting
Endothelial cells
Epithelial cells

## Slide 33
33
Carrier Binding to Endothelium
anchors a carrier to endothelium in the area of interest
provides desirable subcellular addressing
not adversely affected by carrier binding
Adequate level of expression/localization
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
ICAM-1
Fibroblasts
Muscle cells
Comparable levels of expression
BUT
Endothelial cells only are accessible
Endothelial Determinants for Nanocarrier Targeting
Endothelial cells
Epithelial cells

## Slide 34
34
Carrier Binding to Endothelium
anchors a carrier to endothelium in the area of interest
provides desirable subcellular addressing
not adversely affected by carrier binding
Adequate level of expression/localization
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
ICAM-1
Epithelial cells
Fibroblasts
Muscle cells
Comparable levels of expression
BUT
Endothelial cells only are accessible
Endothelial Determinants for Nanocarrier Targeting
Endothelial cells
Cytokine and transporter receptors
Expressed on cells in blood, RES, lymphoid tissues, hepatocytes
Lack of specificity
Not suitable for endothelial delivery

## Slide 35
35
Carrier Binding to Endothelium
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Healthy endothelium
ACE
angiotensin-converting enzyme
APP, membrane-bound aminopeptidase P
PV-1, plasmalemma vesicle-associated protein
ICAM-1
intercellular adhesion molecule
PECAM, platelet-endothelial cell adhesion molecule
Endothelial Determinants for Nanocarrier Targeting

## Slide 36
36
Carrier Binding to Endothelium
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Healthy endothelium
Pathological conditions
V
Ex novo synthesis/ exposure
Re-arrangement
Cell contraction
Increase cell permeability
Access to PECAM, VE-cadherin
Masking
ACE
angiotensin-converting enzyme
APP, membrane-bound aminopeptidase P
PV-1, plasmalemma vesicle-associated protein
ICAM-1
intercellular adhesion molecule
PECAM, platelet-endothelial cell adhesion molecule
exposure of P-selectin from intracellular storage
de novo synthesis of E-selectin and VCAM-1
Endothelial Determinants for Nanocarrier Targeting

## Slide 37
37
Carrier Binding to Endothelium
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Endothelial Cell Adhesion Molecules (CAMs)
Constitutive
PECAM
ICAM-1
Inducible
VCAM-1
E-selectin
P-selectin
Exposed on the surface of activated endothelial cells
Facilitate the rolling phase of the vascular adhesion of leukocytes
Mobilization in sites of inflammation

## Slide 38
38
Carrier Binding to Endothelium
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132
Endothelial Cell Adhesion Molecules (CAMs)
Inducible
VCAM-1
E-selectin
P-selectin
Therapeutic strategy
Blockage using antibodies
Drug delivery using nanoscale systems
Exposed on the surface of activated endothelial cells
Facilitate the rolling phase of the vascular adhesion of leukocytes
Mobilization in sites of inflammation
Constitutive
PECAM
ICAM-1

## Slide 39
39
Cell adhesion molecule (CAM)–mediated endocytosis
ICAM-1 recycling in endothelial cells
Up-regulated and functionally involved in vascular inflammation, oxidant stress, and thrombosis.
ICAM-1-mediated targeting
Pathway for recurrent drug delivery permitting sustained effects
Muro S et al., Blood 2005, 105 (2), 650
ICAM-1 reappears on HUVEC surface after internalization of anti-ICAM nanocarriers

## Slide 40
40
ICAM-1-mediated targeting
Recurrent targeting of anti-ICAM nanocarriers to endothelium
in vitro
TNF-α–activated cells
2 subsequent doses of nanocarriers
Muro S et al., Blood 2005, 105 (2), 650

## Slide 41
41
anti-ICAM-1 immunoliposomes
ICAM-1-mediated targeting
2 hours @ 4°C
Hua S et al., J. Liposome Res. 2011, 21, 95– 105
TNF-α induced ICAM-1 expression and cell binding
50 µm
t= 0
t= 1 h
t= 24 h

## Slide 42
42
anti-ICAM-1 immunoliposomes
ICAM-1-mediated targeting
2 hours @ 4°C
Hua S et al., J. Liposome Res. 2011, 21, 95– 105
TNF-α induced ICAM-1 expression and cell binding
50 µm
t= 0
t= 1 h
t= 24 h
Garnacho C et al., J. Pharmacol. Exp. Ther. 2012, 340, 638– 647
anti-ICAM-1 peptide-functionalized nanoparticles
Fibrinogen
Fibrinogen γ chain
ICAM-1 binding

## Slide 43
43
Carrier Binding to Endothelium
Role of size and hemodynamics
Sialyl lewis a: P-selectin targeting ligand
Charoenphol P et al., Biomaterials 2010, 31, 1392–1402
flow chamber model
IL-1β-activated endothelial cells
30–50% hematocrit
Polymer nanoparticles

## Slide 44
44
Carrier Binding to Endothelium
Role of size and hemodynamics
Sialyl lewis a: P-selectin targeting ligand
Effect of diameter
From 100 nm to 10 µm
Charoenphol P et al., Biomaterials 2010, 31, 1392–1402
0.1
0.5
2
5
10
Particle size (µm)
Particle binding (#/mm²)
flow chamber model
IL-1β-activated endothelial cells
30–50% hematocrit
Wall shear rate 200 s-1
Polymer nanoparticles

## Slide 45
45
Carrier Binding to Endothelium
Role of size and hemodynamics
Effect of diameter
From 100 nm to 10 µm
Charoenphol P et al., Biomaterials 2010, 31, 1392–1402
0.1
0.5
2
5
10
Particle size (µm)
Particle binding (#/mm²)
Effect of wall shear rate
From 200 to 1500 s-1
Existence of a critical wall shear rate
Disruptive hemodynamic forces
0.5
2
5
10
Particle size (µm)
Particle binding (#/mm²)
flow chamber model
IL-1β-activated endothelial cells
30–50% hematocrit
Wall shear rate 200 s-1
Polymer nanoparticles
Sialyl lewis a: P-selectin targeting ligand

## Slide 46
46
Carrier Binding to Endothelium
Role of size and hemodynamics
Effect of diameter
From 100 nm to 10 µm
Charoenphol P et al., Biomaterials 2010, 31, 1392–1402
0.1
0.5
2
5
10
Particle size (µm)
Particle binding (#/mm²)
Effect of wall shear rate
From 200 to 1500 s-1
Existence of a critical wall shear rate
Disruptive hemodynamic forces
0.5
2
5
10
Particle size (µm)
Particle binding (#/mm²)
flow chamber model
IL-1β-activated endothelial cells
30–50% hematocrit
Wall shear rate 200 s-1
Effect of ligand number
From 800 to 2000/µm²
Larger particles need more target molecules to anchor on the cell
Polymer nanoparticles
Sialyl lewis a: P-selectin targeting ligand

## Slide 47
47
Role of hematocrit
Fullstone G et al., Sci Rep 2015, 5, 10649
Carrier Binding to Endothelium
:
Intermediate range of hematocrit could be better for allowing maximum dispersion of nanoparticles towards the edge of the vessel

## Slide 48
48
Geometry and Plasticity: forces acting on particles under flow
Carrier Binding to Endothelium
Polystyrene spheres
elongated particles stretched from the 200 nm spheres
1 µm
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132 and Kolhar P et al., Proc Natl Acad Sci U S A. 2013, 10 (26), 10753-8
Notes: Specifically, polystyrene nanorods (aspect ratio ∼3) functionalized with anti-ICAM showed upward of 3-fold attachment to brain endothelial cells in static cell culture. (271) Higher association of rod-shaped particles with endothelial cells was also exhibited in vivo as anti-ICAM coated rods exhibited ∼2-fold higher accumulation in target tissue (lungs) than that of spheres of identical volume. This was further investigated by coating nanorods and spheres with anti-transferrin-receptor monoclonal antibody. Rods exhibited almost an order of magnitude fold enhancement in attachment to brain endothelium

## Slide 49
49
Geometry and Plasticity: forces acting on particles under flow
Carrier Binding to Endothelium
Polystyrene spheres
elongated particles stretched from the 200 nm spheres
shape change
lateral diffusion of ligands
higher number of productive anchoring engagements
1 µm
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132 and Kolhar P et al., Proc Natl Acad Sci U S A. 2013, 10 (26), 10753-8
Notes: Specifically, polystyrene nanorods (aspect ratio ∼3) functionalized with anti-ICAM showed upward of 3-fold attachment to brain endothelial cells in static cell culture. (271) Higher association of rod-shaped particles with endothelial cells was also exhibited in vivo as anti-ICAM coated rods exhibited ∼2-fold higher accumulation in target tissue (lungs) than that of spheres of identical volume. This was further investigated by coating nanorods and spheres with anti-transferrin-receptor monoclonal antibody. Rods exhibited almost an order of magnitude fold enhancement in attachment to brain endothelium

## Slide 50
50
The Optimal Carrier Avidity and Ligand Density
Carrier Binding to Endothelium
A
B
C
steric limitations competition
multiple binding firm binding
suboptimal targeting
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 51
51
The Optimal Ligand Density
Carrier Binding to Endothelium
Calderon AJ et al., Journal of controlled release. 2011, 150, 37-44
in vivo
in vitro
4100 Ab/μm²
1100 Ab/μm²
Non specific Ab

## Slide 52
52
Multiple targeting: dual functionalization
Carrier Binding to Endothelium
Preferential binding
Combine basal adhesion with binding to low expressed targets
Equal binding
Too similar distribution
NO binding
Scarce expression in the area of interest
Adapted from Howard et al., ACS Nano 2014, 8 (5), 4100-4132

## Slide 53
53
Vascular Targeting: Perspectives
Adequate understanding of biomedical factors
Atheroma
Blood brain barrier
Optimal nanocarrier design
Balanced combination of stealth and targeting features
Relevant models for predictive screening
Quantitative real-time tracing of both carrier and cargo

## Slide 54
Sudong k et al., Lab on a chip 2013, 13, 1489
Perfusable microvascular network
Stroma channel
(with fibroblasts)
Fluidic medium channel
Fibrin gel channel
Endothelial cells
Vasculogenesis
Angiogenesis
Posts : paracrine interaction
Vasculogenesis
Angiogenesis
700 µm
50 µm
Microfluidic devices

## Slide 55
Perfusable microvascular network
Flow-induced endothelial responses
Perfusable and intact lumina
20 µm
20 µm
200 µm
Flow
7 µm beads
F-actin
Endothelial NO synthesis
20 µm
50 µm
Sudong k et al., Lab on a chip 2013, 13, 1489
Static
70 kDa dextran
No leakage
Intact barrier
Microfluidic devices

## Slide 56
Perfusable microvascular network
Wang X et al.,. Lab on a Chip 2016, 16,282; Sobrino A et al., Scientific reports 2016, 6, 1.
Optimised pore design
NO gel leakage
Vasculogenesis, Sprouting & Anastomosis
Microfluidic devices

## Slide 57
Wang X et al.,. Lab on a Chip 2016, 16,282; Sobrino A et al., Scientific reports 2016, 6, 1.
Optimised pore design
NO gel leakage
Vasculogenesis & Anastomosis
Microfluidic devices

## Slide 58
Perfusable microvascular network
Stromal cells in
perivascular position
Basement membrane deposition
Coculture with cancer cells: Vascularized Micro-Tumors
100 µm
100 µm
Drug treatment: cancer or endothelial cell targeting
Suitable for the development of novel treatment with multiple targets
Wang X et al.,. Lab on a Chip 2016, 16,282; Sobrino A et al., Scientific reports 2016, 6, 1.
Ctrl
FOLFOX
Microfluidic devices

## Slide 59
Wang HF et al., ACS Nano 2018, 12, 11600
Central region for trapping tumor spheroids
Steady medium perfusion for culturing endothelial cells
Ovarian cancer cells (SKOV3) spheroids
Confluent HUVEC monolayer
Open top device for nanomedicine screening
Chip Design
Microfluidic devices